## Slide 1
粉末X光衍射图EM算法全谱线拟合
报告人：曹 斌
导 师： 张统一
amorphous diffraction

## Slide 2
Rp=2.070, Rwp=3.218
relative bulk crystallinity ：39.799%
PB form I
Amorphous
halos
Amorphous pattern

## Slide 3
2: a density function
The atom number at the shell :
1: physical model
: an atom
dr
3: the diffraction intensity of a single atom
: the diffraction intensity, mass and charge of electron
：intensity of incident ray
:atom diffraction factor
the angle between the diffraction ray direction and the incident ray
R: the distance between sample and detector
is polarization factor
A ball in 3-d

## Slide 4
Assume there are Z+1 atom contained in the cluster
At a specific moment, we thave
coordinate origin
,one atom
Z atoms
displacement vector
Optical path distance:
Phase distance:
=
: angle between vector and

## Slide 5
The total diffraction intensity of the cluster,
How to calculate atom’s number ?
Assume that the atom is uniform distributed in sapce
We have
We define that :

## Slide 6
The total diffraction intensity of the sample,
is the effective number of atoms in the sample
)
the average atom density per unit volume

## Slide 7
For any given
Term is the integration of left curve
final pattern

## Slide 8
Integral area , A, represents coordination number
Peaks distance, d, represents average atomic distance
d
A